## Slide 1
Update on high-Q cavities at SHINE
Jinfang Chen
SARI / ShanghaiTech, SHINE project
TTC，September 8th，2022

## Slide 2
Introduction
Progress on high-Q cavities at SHINE
  Gradient improvement on N-doped cavities
  Better fast cooling schemes in VT
  High-Q preservation after He-tank welding
Summary
OUTLINE

## Slide 3
High-Q studies at SHINE, based on the SHINE new facilities in the co-built Wuxi platform.
Reports on Jan. 25, 2022
  High-Q achieved with both N-doping and mid-T baking recipes
  At beginning, max gradient limited at around 18.5 MV/m on N-doped cavities
  On single-cell cavity，max gradient was improved by EP reset (~split bulk EP) and re-doping
  Lower Q0 (10%~30%) in SARI VT, likely due to poor flux expulsion
Introduction - Results on the previous TTC meeting (Jan. 25th)
N-doping on 9cell cavities
38 MV/m
~19 MV/m

## Slide 4
Introduction
Progress on High-Q cavities at SHINE
  Gradient improvement for N-doped cavities
  Better fast cooling schemes in VT
  High-Q preservation after He-tank welding
Summary
Outline

## Slide 5
R&D to improve max Eacc for N-doped single cavity
  Cav1(TF63): After 50um EP reset and re-doping at 800C, max Eacc doubled, ~38 MV/m while maintain high-Q.
  Cav2(S02): with same recipe as Cav1, RF performance repeated!
Gradient improvement on single-cell cavities
Admin limit
4.E+10
38 MV/m
~19 MV/m
3.E+10

## Slide 6
Recent progress on N-doped 9cell cavities: Q0>2.8E+10@16MV/m, Eacc>25 MV/m
Q0 difference likely due to different fast cooling at PKU and SARI (improved since May)
Gradient improvement on 9-cell cavities
N-doped 9-cell cavities
~ 8MV/m
Surface treated with SHINE facilities in Wuxi
Same processes applied:
EP 50um reset, acid T≤10℃
Ramp up to 800C, hold 30mins
3 mins N2 injection, 60 mins annealing
EP 10um, acid T≤10℃

## Slide 7
R&D on fast cooling schemes in vertical tests at SHINE: higher thermal gradient for a better flux expulsion.
Now we are able to test cavity of Q0> 4E+10.
N-doped single-cell cavity
Admin limit
~ 25% increased
Better fast cooling schemes in VT
Fast cooling for the VT (5.10)
T-sensors
9.2K

## Slide 8
Four 9-cell cavities treated in Wuxi platform, have been welded with He-tank.
Two midT-baked cavities, high-Q preserved after He-tank welding. The other two N-doped dressed cavities are under test.
High-Q preservation: bare to dressed cavity
Dressed cavities
Bare cavities
(300C/3h)
Mid-T baked 9-cell cavities

## Slide 9
High-Q recipes have been transferred to manufactories, including foreign vendors.
High-Q achieved on the first bare cavities, tested in Shanghai. Cavities will be sent back to vendors for Helium-tank welding.
High-Q: transfers to cavity manufactories
First 2 bare cavities produced by vendor B with High-Q recipes offered by SHINE
2nd cavity produced by vendor A, arrived

## Slide 10
Introduction
Progress on High-Q cavities at SHINE
  Gradient improvement for N-doped cavities
  Fast cooling schemes in VT
  High-Q preservation after He-tank welding
Summary
Outline

## Slide 11
High-Q cavities R&D has been carried out at SHINE, based on the newly constructed infrastructures for cavity surface-treatments, cavity test etc.
Progress achieved on high-Q cavities R&D in the past months, including the N-doping, MidT baking, flux expulsion in vertical test etc. Now, we are able to achieve
  On single-cell cavities: Q0>4.0E+10 @16-21 MV/m, max Eacc >33 MV/m;
  On 9-cell cavities (both N-doping and midT baking): Q0>2.8E+10 @16-21 MV/m, max Eacc >25 MV/m;
  Better fast cooling schemes for high-Q cavity tests;
  High-Q maintaining from bare to dressed cavities;
  High-Q recipes transferred and realized in manufactories.
Next step, the 1st prototype CM with 8 high-Q cavities is in preparation for assembly, including 4 midT-baked cavities from IHEP, 2 midT-baked and 2 N-doped cavities from SARI, and 2 Large-grain cavities (cooperated with DESY) as backup.
Summary

## Slide 12
Thanks for your attention!
References:
Ari D. Palczewski’s talk, High Qo/High gradient at JLab: LCLS-2 HE 3N6 doping, furnace issues and FNAL 75˚C retests, TTC meeting, at TRIUMF, Feb 5th – 8th 2019.
Dan Gonnella’s talk, The LCLS-II-HE R&D Program - New Insights into Improving the Performance of Nitrogen-Doped SRF cavities, IPAC’21
Kensei Umemori’s talk, New results of KEK New results of KEK，TTC meeting, at CERN, Feb 4th 2020.
Feisi HE, et al., Experimental study of simplified mid-T furnace baking at IHEP, Supercond. Sci. Technol. 34 (2021)
  Special thanks
  To Wuxi Creative, OSTEC, HIT, PKU, IHEP, DESY, INFN-LASA, KEK, RI, ZANON and many other cooperative institutions and companies
To everyone in SHINE cryomodule team and cryogenic team, as well as to Zhi Liu’s team in ShanghaiTech University.